## Slide 1: Some thoughts about energy storage modelling in power systems
David Howey and Volkan Kumtepeli
DIGEST Meeting
March 2023

## Slide 2: Why should power engineers care about batteries?
According to Aurora Energy Research*:
1 GW of batteries contracted in UK via capacity market to date
50% of “frequency containment reserve” in Germany covered by batteries in 2018
400 MW batteries deployed 2016-18 in the US
China targets 7 million EVs by 2025
Like it or not, batteries are here, and to control them correctly we need to understand their:
  Dynamics
  Thermal behaviour
  Degradation characteristics

## Slide 3: Why should power engineers care about batteries?
Model fidelity (maybe) matters. Example: optimally control a grid battery to maximise profit on wholesale arbitrage market:
here is ‘the battery
model’
If one assumes the battery is just a simple “bucket for energy”, one may under-estimate the revenue and the costs. Using a more nuanced dynamic battery model including degradation here almost doubles the profit, in our calculations, but is complex.

## Slide 4: Battery modelling – why is it useful?
Design (cell, pack)
  How to predict behaviour of a new
  chemistry
  How do I design electrodes
  How much heat will my cell produce
  How do I design a balancing system
  How do I match cells within a pack
Estimation (e.g. BMS, VSC)
  State of charge (SOC)
  Temperature
  State of health (SOH)
  Power capability
System integration & control (e.g. EMS, VSC)
  What is the efficiency map
  What is the optimal (dis)charge profile
  How long will the batteries last
  What voltages will the inverter see

## Slide 5: Electrochemical devices are all similar
Electrically, in all electrochemical devices (supercaps, fuel cells, flow batteries) there is a voltage source, and there are losses*.
Batteries (e.g. li-ion) are similar, but exhibit transport limitations:
Supercap |  | 
Fuel cell |  | 
Flow battery |  | 
Supercap |  | 
Fuel cell |  | 
Flow battery |  | 
* Ignoring, in this simple model, additional dynamics, and ignoring mechanical losses
Battery |  | 
Battery |  | 
ohmic kinetics diffusion
SOC

## Slide 6: Understanding state of charge in lithium-ion
Cell SOC must be defined against cell open circuit voltage.
Cell OCV is a combination of positive & negative electrode OCV.
Voltage limits are established against each electrode.
These dictate the cell OCV min/max, and hence SOC min/max.
SOC min (full discharge)
SOC max (full charge)
cell Vmax
cell Vmin
+ve electrode
establishes Vmax
-ve electrode
establishes Vmin

## Slide 7: A basic battery model: voltage source + resistor(s)
The terminal voltage is:
The Butler-Volmer equation can be used for and however, assume for simplicity here that it can be linearised. This gives:
How accurate is this?
Actually, not bad, but
we may also like to
model the diffusion
dynamics (<1 Hz).
overpotential of each electrode (i.e. kinetics)
OCV of each electrode (nonlinear function of SOC)
ohmic/ionic losses

## Slide 8: Battery packs may be modelled in a similar manner
So far we have only discussed cell modelling. However most larger systems (EV, grid) include 100s-10000s of cells to form a pack. How do we model this? There are two extremes:
  Model the entire pack as if it’s one big cell.
  Model every cell in the pack
A compromise is to model every (sub)-module as if it was a cell.
In practice ECMs are almost exclusively used for option 1 since they represent average behaviour (could be significant cell-to-cell variations in the pack).
In series connected systems, the equivalent cell model has a resistance and voltage that is the sum of the underlying models:
In parallel connected systems:

## Slide 9: Thermal management is important for devices
Lithium-ion batteries have a limited ideal temperature range; ~20-40 ℃ is optimal.
At lower temperatures, resistance increases, limiting power capability and there is a risk of lithium plating.
At higher temperature, degradation is faster and there are safety issues.
Temperature uniformity within cells and across packs is also important to avoid imbalanced usage – ideally is kept < 5 ℃.

## Slide 10: Temperature strongly impacts performance
Most electrochemical equations include a term (e.g. Nernst, Butler-Volmer); reaction constants, OCV, conductivities and diffusivities also vary with .
We need to understand how much heat is generated and what sort of impact this will have, and how to design an appropriate cooling system.
Li-ion useable capacity decreases with decreasing temperature (top right) due to increased resistance; it also decreases with increased C-rate for similar reasons (bottom right), but not as much as we might think (due to higher temperatures!).

## Slide 11: Lithium-ion batteries degrade with time and use
Copper dissolution and dendrite formation
Transition metal dissolution and
dendrite formation
Solvent co-intercalation and graphite exfoliation
Lithium plating and dendrite formation
SEI decomposition
and precipitation
Binder de-composition and contact loss
Copper cracking
and contact loss
Aluminium
corrosion and contact loss
Aluminium current collector
Binder
Binder
Separator
Carbon
Anode
SEI
Structural disordering
Cathode
Li+
Particle
cracking
Cathodic
surface film
Copper current collector
Internal short-circuit
Particle cracking,
SEI formation
and build-up
Gradual degradation is thought to be caused by build up of negative electrode “solid electrolyte interphase” (SEI) and particle fragmentation. Internal short circuits are also a concern.

## Slide 12: Degradation depends on SOC, temperature..
Data: Mat4Bat project, Reniers, Howey et al. J Power Sources 379:91-102, 2017
Calender ageing Cycle ageing

## Slide 13: Degradation impacts arbitrage revenue using EES

## Slide 14: Discussion points
What energy storage systems should be considered? (possibilities: Li-ion, pumped hydro, flow battery, liquid air, supercaps, [flywheels?])
What are the key energy storage parameters required?
  Two of these: Capacity (MWh), power rating (MW), duration (h)
  Efficiency (charge/discharge) – or losses
  Degradation cost
What cost function(s) do we want to optimize against? (how much do we care about optimal sizing vs. optimal control)
How should one (de)couple the ‘long term’ investment question (e.g. 30 years horizon) with the short term decision making. (This is really a question of how to cost degradation correctly in the short term – short term decisions may impact degradation cost)
What price data to use?

## Slide 15: Background stuff

## Slide 16: Lithium-ion: intercalation within host electrodes
Full cell (2.7–4.2 V vs. Li)
Negative electrode (0.1–1.3 V vs. Li)
Positive electrode (3.5–4.5 V vs. Li)
Lithium-ion batteries are different to most other batteries; the solid electrodes change composition through intercalation, where Li+ is inserted reversibly between the electrode layers.
There is (ideally) no involvement of the solvent in normal cycling.
Above: Intercalation of lithium ions into a graphite electrode
(image: wikimedia commons, public domain)
Li+
Li+
Note: other cathode materials available
C
D
C
D
x, y are SOC of + and - electrodes
Notes: X = fractional occupancy of sites in the lattice

## Slide 17: There are a range of electrode materials available
Graphite: most common negative material (Li2TiO3 also used)
Various lithium-metal-oxide positive materials are used:
graphite negative electrode (SEM)
x1500 mag
NCA positive electrode (SEM)
x1500 mag
Cathode materials | Nominal cell volts (V) | Energy density (Wh/kg) | Power density (kW/kg)
LiCoO2 (LCO) | 3.8 | 80-150 | < 0.5
LiMn2O4 (LMO) | 3.8 | 150-180 | < 2
LiNiCoAlO2 (NCA) | 3.8 | 100-130 | < 1.1
LiNiMnCoO2 (NMC) | 3.8 | 125-200 | < 1.2
LiFePO4 (LFP) | 3.3 | 50-130 | < 2

## Slide 18: Electrolyte and current collectors need to be stable
The electrolyte in a li-ion cell includes a:
  Solvent, which is a non-aqueous organic liquid or polymer because of the reactivity of water with lithium,
  Solute, made up of lithium salt e.g. LiPF6, LiBF4 or LiClO4.
One reason for the upper voltage limit is to avoid oxidation of the electrolyte.
The current collectors are:
  Aluminium is used at the positive electrode since it is stable at high potential although reacts with lithium below 0.6 V (vs. Li).
  Copper is used at the negative electrode (but it oxidises at > 3.2 V vs. Li causing impurities to enter the electrolyte).
Here’s what happen to my old iphone when left uncharged for months.
Image: Wikimedia commons by Mpt-Matthew, CC BY-SA 3.0 licence.
Inside a lithium-ion cell – lithiated electrode material

## Slide 19: Batteries are all about the open circuit voltage (OCV)
Often overlooked, OCV in fact usually dominates the voltage response!
Voltage drops due to internal resistances generally quite small by comparison
Galvanostatic intermittent titration test (GITT) is used to measure open circuit voltage
Small (dis)charge, then a long rest period for cell to relax.
Another technique is “pseudo-OCV” measurement, which is a very low C-rate (discharge) e.g. C/24

## Slide 20: Worked example: Equivalent circuit model
1. Derive a state space model for the battery equivalent circuit shown below assuming the input is current and the output is terminal voltage. 2. Linearise this around some SOC point.
Let’s have the states as and the SOC.
The current
Rearranging,
Also, and

## Slide 21: Worked example: Equivalent circuit model
We can now write this in state space form:
System dynamics are linear, but output equation is nonlinear.
There are two states: the voltage drop across the R//C, and the state of charge. The open circuit voltage is a function of SOC. Linearise around a state of charge giving :
SOC
capacity
linearised OCV
A
B
C
D

## Slide 22: This models diffusion dynamics reasonably well
Observe the battery continuing to generate heat even after the high current pulse is stopped.
voltage
“relaxation”
iR drop

## Slide 23: Thermal equivalent circuits (TECs) are a useful tool
Although there are neat techniques for achieving very low order solutions to the PDE problem, a common approach for thermal modelling is thermal equivalent circuits.
These are “0D” models – heat generation typically lumped into one average term. The idea is similar to the ECMs we used before – but applied to the heat equation.
We have: current source (heat); , capacitance; and , equivalent radial and axial resistances, fitted; , equivalent convection resistances
Averaged internal temperature of cell